## Slide 1: MRI of Ice Formed by Sea Spray
Grant Wilbur

## Slide 2: Motivations
Ice buildup on marine vessels can be very dangerous
Work is being done on computational models for thermal and structural properties of these ices
Some NMR measurements have been made on these ices
No one has done MRI on these sea ices
Notes: We are trying to help the computational physicists with their numerical solutions

## Slide 3: Experiment
Creating simulated sea ice within an MRI scanner
Make measurements!
SPRITE images, T2 , and T1 – T2 mapping

## Slide 4: How Does MRI/NMR Work
NMR (Nuclear Magnetic Resonance) is the phenomenon which allows us to do MRI
  Fairly simple! (if you know some E&M)
MRI is a series of techniques that exploit NMR
  Varying complexity depending on the technique

## Slide 5: NMR Basics
Sample is placed in external magnetic field causing spins to align in z direction.
RF pulse is applied causing magnetization vector to tip into transverse plane.
Once the RF pulse has ended, the magnetization precesses in the transverse plane as it re-aligns with the external field
Visualization of magnetization vector tipping
into transverse plane after application of
RF pulse.

## Slide 7: Specific Challenges
Our apparatus cannot directly detect the spins in ice
T2 Water ≈ 50 – 160ms
T2 Ice ≈ 10us
NMR probe dead time: 40us
Notes: Water T2: 130ms
Ice T2: ~10us

## Slide 8: Structure of Brine-Spongey Ices
Ice created by sprays of salt water are different that ice created by pure water

## Slide 9: Experimental Setup
Water Nozzle
-10⁰C sea water spray
-30⁰C Liquid Nitrogen vapour
5mm Glass tube
Sea Ice buildup

## Slide 10: What Does the Ice Look Like?

## Slide 11: MRI Results
We can determine several things from the MRI data:
  Ice growth as a function of time
  Patterns in the ice structure
Take roughly 2.5 minutes per image

## Slide 12
Notes: 8 clicks
Each image take roughly 4 minutes apart
Each image takes ~2:30

## Slide 13
Notes: 10 clicks

## Slide 14
Notes: 7 clicks

## Slide 15: Experimental Results: T1-T2 Map
Bulk measurement
  No spatial information
Plots of T1 vs T2 reveal information about the environments the spins are in

## Slide 16
T1 = 158ms
T2 = 34ms
T1 = 60ms
T2 = 3.6ms
T1 = 125ms
T2 = 27ms
Notes: Pt 14: T1 = 158ms, T2 = 34ms
Pt 15: T1 = 125ms, T2 = 27ms
Secondary: T1 = 60ms, T2 = 3.6ms
Shorter Relaxation times imply more active energy exchange

## Slide 17: Conclusion
We have obtained spatially resolved structural information about sea ices formed from sea spray
We have made some bulk measurements of these ices which can could be made in-situ

## Slide 18: Acknowledgements
Igor Mastikhin – Supervisor
Florin Marica – Research Scientist
Brian Titus – Machinist
Brian Malcolm – Glassblower